## Slide 1: Cu2Se

## Slide 2
Essay about Cu2Se

## Slide 3
Multiformity and fluctuation of Cu ordering in Cu2Se thermoelectric materials P. Lu, H. Liu, X.Yuan, F. Xu, X. Shi, K. Zhao, W. Qiu, W. Zhang and L. chen, J. Mater. Chem. A, 2015,

## Slide 4
Multiformity and fluctuation of Cu ordering in Cu2Se thermoelectric materials P. Lu, H. Liu, X.Yuan, F. Xu, X. Shi, K. Zhao, W. Qiu, W. Zhang and L. chen, J. Mater. Chem. A, 2015,

## Slide 5
Multiformity and fluctuation of Cu ordering in Cu2Se thermoelectric materials P. Lu, H. Liu, X.Yuan, F. Xu, X. Shi, K. Zhao, W. Qiu, W. Zhang and L. chen, J. Mater. Chem. A, 2015,
S1 Triclinic
S2 Monoclinic
S3 Triclinic
S1x1 Trigonal
Sder1 Monoclinic
Sder2 Monoclinic

## Slide 7
Structure family and polymorphous phase transition in the compounds with soft
sublattice: Cu2Se as an example J. Chem. Phys. 144, 194502 (2016); doi: 10.1063/1.4948609
either trigonal,too
S2,S3,Sder2
Sder1
S1
S1X1

## Slide 11
XRD & Current

## Slide 12
Cathode
Anode

## Slide 13
Cathode
Anode
Maybe Cu(111)
Maybe Cu(200)

## Slide 14: Only heating detected on Anode
Be treated
by 3.5Acurrent
Phase transform

## Slide 15
Detecting Cathode on current&750K
Cannot find (hkl)
dspacing(15.8)=5.4567A
dspacing(36.8)=2.3886A
Cannot compare with anode

## Slide 16
Phase diagram
II Cu2Se

## Slide 17
22:29:28 0.853
22:30:34 0.847
22:19:40 0.8536
For(3.5A_heating_third_3)

## Slide 18
Cathode
Anode
Cu對不到可能沒有長成晶粒
沒加熱峰值還較高

## Slide 19
SEM

## Slide 20
BSE
Origin

## Slide 21
SEM
OM

## Slide 22
SE-anode
500~3000x

## Slide 23
SE-cathode
500~3000x

## Slide 24
SE-middle
500~3000x

## Slide 25
EDS

## Slide 26: Anode

## Slide 27: Cathode

## Slide 28: Middle

## Slide 29
Problems&
improvement

## Slide 30
1.Peak form 10~80 measured ,peak of 13 degree is very high
2.Stable heat dissipation and detecting temperature by Thermocouple
3. Anaerobic condition &improving electric conducting method
4. Do pure heating & heating+conducting (non-equilibrium too)
improvement
5. Precisely measuring time to calculate diffusion(structure changing)
6.氮氣瓶不足噴所有試片(做皮箱)照XRD

## Slide 31: Anode

## Slide 32: Cathode

## Slide 33: Middle